CERTIFICATE OF ANALYSIS

Date:			March 14, 2008

Material:		Aluminum Metal Powder

Lot No.:		ACN2118B

CAS #:			7429-90-5

Customer:		Sung-Bo Corp

Ra-1308 Zoongang Youtong Danzi

Goorobondong 1258, Goorogoo Seoul Korea

Purchase Order No.:	80215

Chemical Analysis:  (%)

Gallium		               <0.0200
Titanium		  <0.0100

Zinc	                            <0.0100

Magnesium	               <0.0100

Manganese	               <0.0100

Copper                             <0.0100

Iron                                   <0.0900

Silicon                              <0.0400

Aluminum                         99.8000 min metals basis

Screen Analysis

FSSS:    	4.3 microns

0.06%               +325 mesh

Average particle size: 	1-5 microns

The above analysis is carried out as part of our internal quality control testing and is based upon our analysis methods.

We do not assume any warranty, liability or risk based on such findings.  Our quality is warranted within the scope of our general sales conditions.

Brenda Lyons

Managing Member