| Cotronics Corporation Proprietary Data Sheet |  |  |  |
| --- | --- | --- | --- |
| Chemical Resistance of Duralco 4538 |  |  |  |
| Ratio | 100 parts resin to 120 parts hardener |  |  |
| Cure Schedule | 16 hours @ 77ºF post cure 3 hours @ 212ºF |  |  |
| Sample Size | 3" x 1" x 0.125" |  |  |
| Immersion Time | 7 Days | 28 Days | 120 Days |
| Chemical | %Wt. Chg. | %Wt. Chg. | %Wt. Chg. |
| Sulfuric Acid, 30% | 1.81 | 3.61 | 7.9 |
| Sulfuric Acid, 3% | 1.9 | 4.03 | 9.38 |
| Hydrochloric Acid, 36% | 3.54 | 6.11 | 15.3 |
| Hydrochloric Acid, 10% | 2 | 4.11 | 9.24 |
| Nitric Acid, 40% | D |  |  |
| Nitric Acid,10% | 2.21 | 4.69 | 10.6 |
| Ammonium Hydroxide, 28% | 0.56 | 1.37 | 3.1 |
| Acetic Acid, 25% | 10.86 | D |  |
| Ethyl Alcohol, 95% | 1.49 | 3.03 | 6.45 |
| Acetone | 4.28 | 10.5 |  |
| Ethylene Dichloride | 10 | D |  |
| Toluene | 0.03 | 0.1 | 0.81 |
| Sodium Hydroxide, 50% | 0.01 | 0 | 0.05 |
| Sodium Hydroxide, 10% | 0.48 | 1.03 | 2.23 |
| JP 4 Fuel | 0.03 | 0.04 | 0.22 |
| Citric Acid, 10% | 0.71 | 1.48 | 3.24 |
| Chromatic Acid, 40% | -1.6 | -6.43 | -19.8 |
| Distilled Water | 0.64 | 1.36 | 3.11 |
| Note D designates that the product decomposed |  |  |  |
| Disclaimer: |  |  |  |
| Information that is supplied is not to be taken as a warranty or representation for which |  |  |  |
| Cotronics Corp. Assumes legal responsibility. It is offered solely for your consideration, investigation |  |  |  |
| and verification. All risk of use singly or in combination with other products, whether or not in |  |  |  |
| accordance with the instructions, directions or suggestions is borne by the user. |  |  |  |